## Slide 1: Optics of a single Homogeneous and Isotropic Layer

## Slide 2: Electromagnetic Treatment
For the homogeneous and isotropic media, the whole structure can be described by

## Slide 3: Electromagnetic Treatment
We assume that a plane wave is incident from the left, the electric field vector can be written as

## Slide 4: Electromagnetic Treatment
For s wave, the electric field E(x) is Ey, and Hz can be obtained by Maxwell equations.

## Slide 5: Electromagnetic Treatment
Imposing the continuity of Ex and Hy at the interface x=0 and x=d leads to

## Slide 6: Electromagnetic Treatment
The Fresnel reflection and transmission coefficients of the dielectric interfaces for s waves as

## Slide 7: Electromagnetic Treatment
The transmission and reflection coefficients can be written as
where

## Slide 8: Electromagnetic Treatment
A similar electromagnetic analysis for the p wave leads to exactly the same expressions for the transmission and reflection coefficients.

## Slide 9: Airy’s Formulations
The transmission and reflection coefficients can also be derived by summing the amplitudes of successive reflection and refractions.

## Slide 10: Airy’s Formulations

## Slide 11: Airy’s Formulations

## Slide 12: Airy’s Formulations
Substituting φ+π for φ in above expressions, we obtain

## Slide 13: Airy’s Formulations
In the limit when the thickness of the layer becomes zero, the reflection and transmission coefficients should become those of the interface between media 1 and 3.

## Slide 14: Airy’s Formulations
The presence of a half-wave layer with φ=π does not affect the reflection and transmission of light except for a possible change of sign.

## Slide 15: An Alternative Derivation
At the interface x=0, these are two incoming waves and two outgoing waves. The amplitudes of these waves are related by

## Slide 16: An Alternative Derivation
At the interface x=d, these is only one incoming wave and two outgoing waves. The amplitudes of these waves are related by

## Slide 17: An Alternative Derivation
By eliminating A, C, and D, we obtain

## Slide 18: Transmittance, Reflectance, and Absorptance
Reflectance is defined as the fraction of energy reflected from the dielectric structure and is given by
Reflectance is meaningful only when medium 1 is nonabsorbing.
If medium 3 is also nonabsorbing, the transmittance is given by
The factor corrects for the difference in phase velocity.

## Slide 19: Transmittance, Reflectance, and Absorptance
Absorptance, which is defined as the fraction of energy dissipated, is given by
A = 1 - R - T

## Slide 20: A Thin Film on a Substrate